## Slide 1: Interaction of material poles and optical poles in different systems

## Slide 2
Theory

## Slide 3
Coupled Damped Oscillator Model
Exciton and cavity mode coupling
- cavity mode
- material pole (exciton)
g-the exciton-cavity coupling rate
- the induced polarization of the material pole
C. Carlson et al.,
Phys. Rev. B 104, 125424 (2021)

## Slide 4
Core-shell particle
Fabry-perot cavity
RSE vs material poles
E. A. Muljarov and T. Weiss, Optics Letters, 43, 9, 1978-1981 (2018)
E. A. Muljarov and W. Langbein, Phys. Rev. B 93, 075417 (2016)
– curl Maxwell’s equations in matrix form
where is material matrix,
,
Notes: We specialize in exploring various optical systems such as core-shell particles and Fabry-Pérot cavities. To understand their optical properties, we begin by calculating parameters like reflection or absorption coefficients (for Fabry-Pérot cavities) or scattering and absorption coefficients as a function of parameters such as frequency. As a second step, we perform Eigenmode Analysis to interpret the results more comprehensively and gain deeper insights into the system's behavior

## Slide 5
RSE vs material poles – system of equations
Resonant-state expansion:
overlap electromagnetic mode and induced polarization of material pole
From the definition of :
(
1st equation:
2nd equation:
Notes: We specialize in exploring various optical systems such as core-shell particles and Fabry-Pérot cavities. To understand their optical properties, we begin by calculating parameters like reflection or absorption coefficients (for Fabry-Pérot cavities) or scattering and absorption coefficients as a function of parameters such as frequency. As a second step, we perform Eigenmode Analysis to interpret the results more comprehensively and gain deeper insights into the system's behavior

## Slide 6
where ,
,
System of equations Matrix equation
- wavenumber of i-th optical pole
- p-th material pole
Size of blocks and is (
Linear eigenvalue problem

## Slide 7
RSE
Single mode approximation and 3 material poles
Extended coupled oscillator model
M. Balasubrahmaniyam et al.,
Phys. Rev. B 103, L241407 (2021)
There is an additional shift in the first diagonal element.
- overlap between the n-th electromagnetic mode and the induced polarization of the p-th material pole

## Slide 8
Results

## Slide 9
Result – 3 material poles
N=11 optical poles In the basis there are 2N-1 terms (including –conj(ki))
Air
SURMOF (no mat. poles)
Air
SURMOF

## Slide 10
Result – 1st material pole
N=11 optical poles In the basis there are 2N-1 terms (including –conj(ki))
Air
SURMOF (no mat. poles)
Air
SURMOF

## Slide 11
Artificially increasing the oscillator strength
N=11 optical poles In the basis there are 2N-1 terms (including –conj(ki))
Air
SURMOF (no mat. poles)
Air
SURMOF

## Slide 12
Result – Silver slab
N=11 optical poles In the basis there are 2N-1 terms (including –conj(ki))
Air
SILVER (no Drude poles)
Air
SILVER

## Slide 13
Plasmon-exciton-polariton and RSE - Intermediate step
N=11 optical poles
Thickness of 1st Silver layer = 0.01 um
Thickness of 2nd Silver layer = 0.03 um
Fabry-perot cavity
SILVER (no Drude poles)
SURMOF (no mat. poles)
SILVER (no Drude poles)
SILVER
SURMOF (no mat. poles)
SILVER

## Slide 14
Plasmon-exciton-polariton and RSE
N=11 optical poles
Thickness of 1st Silver layer = 0.01 um
Thickness of 2nd Silver layer = 0.03 um
Fabry-perot cavity
SILVER (no Drude poles)
SURMOF (no mat. poles)
SILVER (no Drude poles)
SILVER
SURMOF
SILVER

## Slide 15
Plasmon-exciton-polariton and RSE
N=11 optical poles
Thickness of 1st Silver layer = 0.01 um
Thickness of 2nd Silver layer = 0.03 um
Fabry-perot cavity
SILVER (no Drude poles)
SURMOF (no mat. poles)
SILVER (no Drude poles)
SILVER
SURMOF
SILVER

## Slide 16
Сoupling of SURMOF poles and optical modes of the silver cavity
N=3 optical poles
Fabry-perot cavity
SILVER (no Drude poles)
SURMOF (no mat. poles)
SILVER (no Drude poles)
SILVER
SURMOF (no mat. poles)
SILVER
SILVER
SURMOF (1 mat. pole)
SILVER

## Slide 17
Сoupling of SURMOF poles and optical modes of the silver cavity
SILVER
SURMOF (no mat. poles)
SILVER
SILVER
SURMOF (1 mat. pole)
SILVER
Matrix
Matrix
- this matrix describes the coupling between the optical modes of the silver cavity and the SURMOF pole

## Slide 18
Single mode approximation:
Under this approximation, the construction of the matrix from the RSE is very similar to the Hamiltonian from the extended coupled oscillator model.
Basis size:
In practice, including just 10-20 resonant states in the RSE expansion is sufficient to achieve accurate results.
SILVER-SURMOF-SILVER workflow:
Calculations proceed in three steps: bare non-dispersive dispersive SILVER coupling to SURMOF poles.
Summary

## Slide 19
Сoupling of SURMOF poles and optical modes of the silver cavity